## Slide 1: The future of solid-state transistors
Jörgen Olsson
Uppsala University
Sweden

## Slide 2: Outline
Development of RF-LDMOS
High-power transistor options
  VMOS
  LDMOS
  GaN
Development trend
Summary

## Slide 3: What is a DMOS? Double-diffused MOS
LDMOS
  Lateral double-diffused MOS
  Short channels
VDMOS
  Vertical double-diffused MOS
  Mostly for high power

## Slide 4: History of LDMOS
1969 – the first LDMOS was presented
1972 – the LDMOS as a microwave device was presented
Switching devices
  Power supplies
  Motor controls
  etc.....
From mid-90‘s – Base station applications
  NMT, GSM, 3G, LTE, 4G (900 MHz-3 GHz)
  NXP (Philips), Freescale (Motorola), Infineon (Ericsson)
Other applications, such as S-band radar etc.

## Slide 5: RF-LDMOS 28V
Major development has been with focus on parameters important for mobile communications, such as gain, efficiency, linearity, increased operation frequency.
Other advantages: high reliability, low-cost package with ground on chip back-side (low inductance and resistance)

## Slide 6: Infineon, 7th generation LDMOS
p+ sinker
Faraday shield
source contact
drain
contact
gate
channel
LDD region
Channel doping by lateral diffusion.
p+ sinker contacts source to backside for low inductance and good rf grounding.
Lightly doped drain (LDD) region for high breakdown voltage
Faraday shield for low Cdg feedback capacitance, reduced hot-carrier injection and optimized breakdown voltage

## Slide 7: Infineon, 8th generation LDMOS
Silicided gate
Thin field plate
Source runner
Au metallization
Low stress ILD
60 um die thickness

## Slide 8: Cross-section of Freescale LDMOS
source: Motorola/Freescale

## Slide 9: NXP LDMOS technology
Vsupply= 28-32 V
Vbd = 70 V
ft = 12 GHz
0.4 um gate length
25 nm gate oxide
Source Contact
P- substrate
P - substrate
P-type
P-well
N+
SN
P-sinker
shield
N+
Source
Drain
Gate
n- drain extension

## Slide 10: Example: 100 W transistor
Drain
Gate
Inshing MOS-
Capacitor
LDMOS-die
Prematch MOS-
capacitor
NXP
BLF6G38-50
Advantage: on-chip matching

## Slide 11: LDMOS for high power
LDMOS for 28-32 V are the most developed due to their use in cellular infrastructure.
Available up to around 400 W and <3GHz
Some limitations are the efficiency and the thermal management

## Slide 12: VDMOS – for high power
Available at high voltages but generally have lower performance than similar LDMOS.
Around 500 W
Disadvantage is that drain is on backside meaning more expansive package solution and worse thermal management.
Also higher feed-back capacitance.

## Slide 13: Alternative semiconductors

## Slide 14: GaN RF power
Due to its better semiconductor properties GaN has the potential to drastically increase RF performance.
Higher supply voltages possible giving higher output power, which is perhaps the most important advantage
The HEMT (high electron mobility transistor) is most common and using a heterojunction structure with 2D electron gas as the current conducting channel

## Slide 15: GaN technology
Hetero structure grown on different substrates:
  Si: lower cost, bigger wafers, but greater mismatch and thermal limitations
  SiC: higher cost, but otherwise better performance (SiC good thermal conductor)
GaN technology may require non-planar technology, such as air-bridges

## Slide 16: GaN performance
Impressive performance has been demonstrated
However, technology still not mature and fully reliable for cellular applications
Drift, charge effects and other phenomenon make the transistor not stable
GaN transistors for pulsed power up to around 500 W @ 50 V are available for frequencies up to 1.5 GHz, but efficiency not that great yet.

## Slide 17: Development trends
The use of e.g. SMPA in cellular, motivated by higher efficiencies, has driven technology towards higher supply voltages
Present 28 V not easily scaled to higher voltages – new concepts may be needed
Major players, such as NXP, Freescale and Infineon now have 50 V LDMOS technology, mainly targeting applications outside the cellular infrastructure

## Slide 18: 50 V LDMOS performance
Typically, increased power density and lower output capacitance is obtained with 50 V compared to 28 V LDMOS technology.
Maximum operation frequency around 3 GHz
Maximum output power above 1kW at rather high efficiency, but at lower frequency < 1 GHz
Excellent ruggedness for large mismatch conditions and > 105 years MTTF at T>200 C

## Slide 19: Going for even higher voltages
Switch LDMOS used for RF-LDMOS with small modifications
Lateral diffusion of p-base -> short channel 0.3 mm
Long poly-gate -> low gate resistance
Long drift region -> high breakdown voltage
channel
Critical regions for high electrical field

## Slide 20: Double RESURF LDMOS
Buried p-top (formed with high energy implant) =>
  more effective drift region depletion (RESURF) =>
  higher drift region (n-well) doping =>
  lower resistance for almost preserved BV =>
  higher drive current
channel

## Slide 21: Double RESURF
Buried p-top assists in depleting the n-well. Very sensitive to the p-top dose. However, about 30 % lower on-resistance is possible for the same BV
Low dose
Optimum dose
High dose

## Slide 22: Enhanced dual conduction layer LDMOS
channel
N-top at surface =>
  Even higher current for preserved BV
  Also changes the field profile at the gate
  (which affects reliability, fT roll-off etc.)

## Slide 23: Excellent results
Developed, UU in collaboration with Comheat Microwave AB, a novel LDMOS transistor with high on-current (170 mA/mm) and high breakdown voltage (>150 V).
World-record RF performance:
2W/mm at 1 GHz, 70 V
>1W/mm at 3.2 GHz, 50 V
Device design:
Expertise in device physics
and TCAD
Device fabrication:
Test structures at MSL
RF-power devices at foundry
Evaluation:
Full electrical characterization
Industrial evaluation

## Slide 24: High performance RF-LDMOS - next generation
BOX
D
S
G
Next generation LDMOS targeted for high efficiency SMPA and pulsed radar
For SMPA:
  f  1/(Cout x RON)
  P  VDD2
SOI results in lower Cout and lower RON - 16x improvement possible!
Current development is targeted at implementation on SOI and hybrid substrates, with extremely high performance predicted; ION>600 mA/mm (>500 mA/mm already demonstrated) and low output capacitance, making SMPA applications above 3 GHz possible. Also suitable for applications in harsh environments (high-T, rad hard etc.)
SOI
Silicon-on-Insultator
substrate

## Slide 25: LDMOS on SiC hybrid substrate
LDMOS on Si/SiC hybrid substrate results in further improvements
S.I. substrate eliminates Csub
Bond pad/wire cap eliminated
Better thermal handling
SMPA at even higher frequency possible or
Higher output power level
BOX
D
S
G
SiC

## Slide 26: Si/SiC hybrid substrates - proof of concept
Defect free 150 mm hybrid substrates manufactured as well as electrical and thermal devices and compared to SOI reference
Si–poly-Si–poly-SiC
Si–(poly-Si)–SiC
SOI
Hybrid substrate has 2-3x higher heat conductivity than SOI. c-SiC slightly better than poly-SiC
SiC
SiC/10um diamond
First ever LDMOS demonstrated on Si/SiC. Ideal transistor behavior with better than or equivalent performance as SOI. No difference in GOI or bulk and inversion mobility. Superior RF performance. Currently in foundry manufacturing (Comheat, VTT)
Simulation show further improvent possible by integrating heat-spreading diamond layer

## Slide 27: Summary
Present commercial 50 V LDMOS technologies provide output power > 1 kW
GaN is in fast development and already > 500 W is available. Maturity and thermal management are issues to address
Silicon (and GaN) can be developed to higher voltage, i.e. power levels
Substrate engineering (SOI and Si/SiC) may be necessary for thermal management and high efficiencies (reduced parasitics)

## Slide 28: Acknowledgments
Some material shown with courtesy of: