## Slide 1
Vittorio Marinozzi
3rd International Workshop of the Superconducting Magnets Test Stands
June 11th, 2019
Electrical integrity of magnets and coils

## Slide 2: Introduction
Before operating magnets and coils, it is important to verify electrical integrity
  Presence of short circuits can damage magnet, coils, equipment, and can be a safety hazard
After construction and before operation of coils/magnets, it is important to verify electrical integrity with dedicated electrical tests

## Slide 3: Introduction (2)
Coils are subject to risk of different kind of short circuits
  To ground
  Turn-to-turn
  Layer-layer
  To floating parts (pole...)
  Diagnostic wires (ground)
  …
Several tests can be performed to mitigate the risk of having shorts during operation
  High-voltage hipotting
  Impulse test
  Electrical measurements

## Slide 4: AUP HiLumi experience
During production of the AUP / HiLumi MQXFA coils, we perform several electrical checkouts, in order to mitigate electrical risks

## Slide 5: Reference document

## Slide 6: Coil electrical design

## Slide 7: Coil in the magnet

## Slide 8: Tests that we perform on QXFA coils
Impulse test
  To verify absence of turn-turn shorts
  Both polarities
  From 1 kV to 2.5 kV, 500 V steps
High voltage Hipots
  Details later
Electrical measurements
  Inductance (20 Hz , 100 Hz, 1000 Hz), resistance, voltage taps
  Repeated at each stage of the coil fabrication
  We have ranges based on past coils measurements

## Slide 9: Test sequence during coil/magnet fabrication
Pre-fabrication: heater traces tested at 3700 V
After winding, curing, reaction, trace installation, impregnation: electrical measurements
After impregnation: HiPot, impulse test
After shipping: HiPot, impulse test, electrical measurements
After magnet assembly: HiPot, impulse test, electrical measurements
The sequence of tests with details is referenced on US-HiLumi-doc-956 and US-HiLumi-doc-521

## Slide 10: Impulse test example (QXFA115)

## Slide 11: Impulse test example (QXFA108)
High frequency, sign of intermittent short

## Slide 12: Hipot values
Golden rule:
  Vhi-pot (4.2 K) = 2 * Vpeak + 500 V
  Vhi-pot (warm) = 2 * Vhi-pot (4.2 K)
  Vpeak from simulations in nominal conditions

## Slide 13: Hipot values (2)
Warm:
  Coil to ground: 3680 V
  QH to coil: 3680 V
  Coil to pole: 500 V
  Coil to end-shoe: 1000 V
  QH to end-shoe (OL): 2500 V
  IL End-shoe to OL end-shoe: 1000 V
Cold (in the test station):
  Coil to ground: 1840 V
  QH to coil: 2300 V
Max leakage current: 1 μA

## Slide 14: Discussion on heater-to-coil voltage
MQXFAP1 (first MQXFA 4 m long prototype) test has been interrupted, due to a short to-ground caused by a short heater-to-coil
This is a single event, due to a weakness of the coil. However, we want to improve our QC in order to mitigate risks

## Slide 15: Peak heater to coil voltages
Peak heater to coil voltages occur after a quench event
  Coil become resistive
  Dump resistor circuit is opened
  Heaters are fired
  CLIQ unit is fired
We should design the electrical tests in order to reproduce as close as possible the conditions that occur during a quench

## Slide 16: What happens during a quench?
Both coil and heaters become hot
If heater-to-coil insulation is damaged, helium superfluid that filled the crack becomes hot as well
  Temperature increase  Pressure increase
Worst situation for the peak voltage could occur at temperature different than liquid helium or room temperature
We would gain from test stations able to test magnets/coils at different sets of temperature and helium pressure

## Slide 17: Example: MQXFA peak heater-to-coil voltages
MQXFA Peak Heater-to-Coil Voltage
Worst situation, interesting to test coils in this condition, at different helium pressures

## Slide 18: Proposal for heater to coil hipot (under discussion)
Take worst combination voltage/temperature, and make a test at 20% higher value
  450 V MQXFA @ 100 K
  800 V MQXFB @ 100 K
  Scale values at room temperature (250 V MQXFA, 450 V MQXFB)
Helium pressure: 1 bar
  Provides margin at 100 K
  Expected pressure at 100 K: > 10 bar (HiLumi-doc-921)

## Slide 19: Conclusions
Checking electrical integrity of coils is important to operate safely magnets and coils, avoiding damages of coils and equipment
During the production of the HiLumi AUP MQXFA coils/magnets, we perform a sequence of electrical checkout to ensure quality
  Well referenced QC procedures and, and clear criteria
Improvement of Quality Control on heater-to-coil tests is under discussion
  Ability of controlling temperature and pressure of helium in test stations would be helpful to improve coil/magnet QC