## Slide 1: Future directions: Challenges of facilities/magnets
E. Todesco
Magnets, Superconductors and Cryostats Group (CERN)
Thanks to Marta, Sandor, Franco, Stoyan, Tatsu, Kevin, Roger, Gerard, and many others for feedback and discussions
12 June 2019 - Uppsala

## Slide 2: THE HL-LHC IR REGION MAGNETS
100 magnets of 11 different types, done via 6 collaborations
To be ready by 2024

## Slide 3: SUMMARY
Techanical challenges
  Training
  Insulation
  Protection
  The brave new world of HTS
Managerial challenges
  Communication
  Training (of people)
  Flux of work
  Flexibility – testing also «other magnets»

## Slide 4: TECHNICAL CHALLENGES
Notwithstanding all efforts to eliminate training (design features as CCT, removable pole) …
  Training is relevant, and it is still there
  Not only in Nb3Sn, but also in Nb-Ti
Quench performance is still the main issue for high current density magnets for accelerators
Training of D1 short model
(T. Nakamoto, et al.)
Training of D2 corrector (CCT)
(G. Kirby, et al.)

## Slide 5: TECHNICAL CHALLENGES
Training mechanism is only partially understood and all instrumentation is necessary
  Voltage taps (in model and prototypes, but in principle not for series magnets)
  Quench antennas for longitudinal localization – looks to me that this is not a routine instrument
  Other, such as acoustic emissions (for the moment still exotic)

## Slide 6: TECHNICAL CHALLENGES
For Nb3Sn magnets are sometimes limited by instabilites
  The nightmare of reverse behaviour
    Better performance with higher ramp rates/ higher temperature
  Important diagnosis tools: be able to make high ramp rate, and higher temperatures in a controlled mode
Instabilities and reverse behaviour in MQXFS3 (H. Bajas et al.)

## Slide 7: TECHNICAL CHALLENGES
For Nb3Sn magnets there are additional points
  A relevant new tool is the VI measurements of order of nV, giving anticipation on quench and degradation
  Here very high sensitivity is a must (nV!)
V I measurements in 11 T short model 109 (G. Willering et al.)

## Slide 8: TECHNICAL CHALLENGES
Protection: CLIQ (G. Kirby, et al.) is becoming a standard tool
  This new technology is being applied in US (FNAL and BNL) and at CERN to protect the triplet
  It is routinely used without major issues in 3 test stations

## Slide 9: TECHNICAL CHALLENGES
Insulation can be an issue for test stations
  In many cases reaching the required level of voltage test (above 1 kV) is a challenge of the test station
    In HL-LHC happened for instance in LASA, KEK
    High voltage levels imply a verification of all the chain from the warm powering to the magnet
Controlled cool-down and warm-up
  The issue of the maximal gradient during cool down and warm up and how to control it is non trivial, especially for Nb3Sn magnets
    Recent issues with 11 T tests

## Slide 10: HTS: A BRAVE NEW WORLD ?
With HTS we enter a radically different domain in terms of training and protection
  Very large temperature margin, current sharing regime above the short sample limit, possiblity to « see » the quench well before
  Training could disappear from our dashboard of issues
Quench onset in Feather2 (J. van Nugteren et al, IEEE TAS 28 (2018))

## Slide 11: SUMMARY
Techanical challenges
  Training
  Insulation
  Protection
  The brave new world of HTS
Managerial challenges
  Communication
  Training (of people)
  Flux of work
  Flexibility – testing also «other magnets»

## Slide 12: MANAGERIAL CHALLENGES
The flow of magnets to be tested is very discontinous
  It follows the timeline of the projects
  This poses challenges for small test stations, or test stations strongly dependent on one project
    Organization
    Training of people
    Maintenance of instrumentation

## Slide 13: MANAGERIAL CHALLENGES
Communication
  The sharing of the data is always a relevant issue
    General approach of sharing post processed data
  Immediacy of the communication is also a strategic problem
    In some cases decisions have to be taken very rapidly
  Test reports !

## Slide 14: MANAGERIAL CHALLENGES
Schedule
  Even though the time scale of our projects is of the order of 10 years, we are constantly fighting against time
  Availability and efficiency are particularly critical for HL LHC project, that has very small series of magnets (practically, one is always in prototype phase)
  Continuous streamlining request to remove the unnecessary tests and give priority to the relevant one
    Doing everything is impossible
    Very good contact between design, construction and tes team is needed

## Slide 15: THANKS